## Slide 1
P-80 Rubber Assembly Lubricants
Providing Assembly and Cleaning Solutions since 1923
160811

## Slide 2
Company Overview
International Products Corporation (IPC), incorporated in 1923, manufactures specialty chemicals. IPC has over 90 years experience manufacturing and selling precision cleaners and formulated lubricants to various industries.
All products are manufactured in the U.S.A. at their New Jersey headquarters and are available worldwide. International Products Corporation is an ISO 9001:2008 Certified Company
Distributor Locations
Company Headquarters

## Slide 3
Why Use Rubber Assembly Lubricants
  Rubber materials are inherently difficult to install, remove, or otherwise manipulate – even when wet
    Common Assembly Problems Include
        Rolling O-rings
        Uneven cuts
        Misaligned parts
        Damaged parts
        Sore muscles, worker injury
          Repetitive Stress Injury (RSI)

## Slide 4
Reduce Installation Force
  Reduce surface tension
  Slide parts into place easily, providing a tight fit
Achieve Closer Fits
  Design lower tolerance parts
  Increase torque installation
  Temporary lubrication only ─ resulting in a tight fit
Improve Product Performance
  Reduce or eliminate damage to parts
Increase Production Rates
Allow for faster, more productive assembly
A Rubber Lubricant Should:

## Slide 5
Avoid Injuries
  Avoid musculoskeletal, slippage, and repetitive stress related injuries
  Safe to handle
Reduce Rejects
  Must be compatible with surfaces and liquids with which it may come in contact
  No shrinking, softening, swelling, crazing or rusting
  Should dry without residue when properly applied
Environmentally Friendly, Easy to Dispose
A Rubber Lubricant Should:

## Slide 6
Items to Consider when Choosing a Lubricant
  Surface compatibility
    Metals
    Elastomers
    Plastics
  Dry time
  Lubricant conductivity
  Chemical composition concerns

## Slide 7
Types of Commonly Used Lubricants
Soap and Water
Alcohol
Kerosene
Silicone
Petroleum Oil
Petroleum Jelly
New, ester based, biodegradable choices

## Slide 8
  Solvents (e.g. alcohol) Provide poor lubrication, are flammable with high VOCs and are a safety risk
  Soaps and detergents provide a nominal amount of lubricity but reactivate when wet
  Petroleum distillates lubricate, but are often not compatible with surfaces – and are not temporary
  Ester technology provides excellent reduction in friction, temporary lubrication, environmental and worker safety.
%
Efficiency of Lubricants
Comparison of Lubricants
Formulated Water and Ester Emulsion
Formulated Surfactant Based Lubricant
Soap and Water
Petroleum Oil Based Lubricant
Solvents
%

## Slide 9
Typical Rubber Assemblies
    Belts
    Boots
    Bumpers
    Bushings
    Diaphragms
    Fasteners
    Foam grips
    Gaskets
    Grommets
    Hoses
    Insulators
    Mounts
    O-rings
    Plugs
    Rubber moldings
    Seals
    Sleeves
    Threaded connectors
    Tires
    Rubber washers
    Wire harnesses
    …And hundreds of other rubber and soft plastic parts

## Slide 10
Why Use a Specially Formulated Temporary Rubber Lubricant?
  Consistent Composition
  Low Impurities
  Green Chemistry
  Favorable Compatibility
    Petroleum-based products have a tendency to swell certain rubbers and damage plastics
    Soap and water can cause corrosion and future slippage when wet
    Silicon interferes with coating and painting

## Slide 11
  Why esters?
    Molecular structure is conducive to lubrication
      Structurally flexible functional groups; C-O-C bonds can rotate easier than other functional groups
    Performance over volume ─ a little goes a long way
    Do not fluoresce
      Improving leak test results
Formulated Temporary Rubber Assembly Lubricants

## Slide 12
Formulated Temporary Rubber Assembly Lubricants
  Innovative Emulsion Technology
    Synthetic esters blended with water
  Why an emulsion?
    Synergy!
      Emulsion has better lubrication than esters by themselves
      Reduces surface tension of rubber to allow esters to get into all of the nooks and crannies of the rubber
      Allows a thin layer of esters to coat the rubber for hydrodynamic lubrication
      Temporary lubrication – Once water evaporates, ester film absorbs into elastomer

## Slide 13
ESTER BASED TEMPORARY RUBBER ASSEMBLY LUBRICANTS | TRADITIONAL RUBBER ASSEMBLY LUBRICANTS
Provide lubricity and reduce friction. | Provide lubricity and reduce friction.
Temporary lubrication, once dry will not reactivate, resulting in tight fitting parts. | Continual lubrication, can reactivate in presence of water ─ resulting in problems with quality and consistency of finished product.
Will not dry out rubber or corrode metal parts. | Can dry out rubber and corrode metal parts.
Any residue is non-conductive. | Many additives are conductive.
Non flammable, negligible VOCs. | May contain VOCs. May be flammable.
Excess lubricant washes away easily. | In some cases may be difficult to wash away excess lubricant.
Compatible with elastomers and plastics. Will not swell rubber. | May not be compatible with elastomers and plastics. Can swell rubber.
Treated surfaces can be coated and painted afterwards. | May interfere with downstream coating and painting processes.
Environmentally friendly and non-hazardous. | Environmental and health hazards can exist.
Lubricant Comparison Chart

## Slide 14
P-80® Emulsion Temporary Rubber Assembly Lubricant
P-80® THIX Temporary Rubber Lubricant Gel
P-80® Grip-it Quick-Drying Temporary Rubber Assembly Lubricant
P-80® RediLube Temporary Rubber Assembly Lubricant
P-80® Emulsion IFC* Temporary Rubber Assembly Lubricant
P-80® THIX IFC* Temporary Rubber Lubricant Gel
*IFC for Incidental Food Contact Applications. Registered with NSF for use in USDA H1 applications and meet FDA regulation 21 CFR 178.3570 which controls lubricants in contact with food surfaces.
IPC’s P-80® Family of Temporary Rubber Assembly Lubricants

## Slide 15
 | P-80® EMULSION | P-80® THIX | P-80® GRIP-IT | P-80® REDILUBE | P-80® EMULSION (IFC) | P-80® THIX (IFC)
Viscosity, cps @ 25° C | 150 | 12,000 | 20 | 20 | 150 | 15,000
Biodegradable | Yes | Yes | No | Yes | Yes | Yes
Reduction of Friction | ~70% | ~70% | ~40% | ~55% | ~70% | ~70%
Estimated minimum dry time | 1 hour | 2 hours | 20 minutes | 20 minutes | 1 hour | 2 hours
pH (neat) | 7.5 to 9.5 | 7.5 to 9.5 | 9.8 to 11.3 | 7.5 to 9.5 | 7.5 to 9.5 | 8.2 to 9.4
Appearance | Milky white to beige | White to beige gel | Clear, colorless | Milky white to light yellow | Milky white to beige | White to beige gel
Shelf life | 2 years | 2 years | 2 years | 1 year | 2 years | 2 years
P-80® Temporary Rubber Assembly Lubricant Product Specifications

## Slide 16
Lubrication over time chart

## Slide 17
  REDUCTION OF FRICTION
P-80 Emulsion
P-80 THIX
P-80 Emulsion (IFC)
P-80 THIX (IFC)
P-80 RediLube
P-80 Grip-it
  ESTIMATED MINIMUM DRY TIME
P-80 Emulsion
P-80 THIX
P-80 Emulsion (IFC)
P-80 THIX (IFC)
P-80 RediLube
P-80 Grip-it
20 Minutes
20 Minutes
2 Hours
2 Hours
1 Hour
1 Hour
Lubrication -vs- Drying Time
Reduction of friction data was created using a force gauge comparing both the dry and wet removal forces of hoses on an end cap. The equipment used; Mecmesin AFG 1000N force gauge, a Mecmesin Multi Test 2.5-d automatic test stand, and accessories to hold the cap and hose in place. The test stand is set to a fixed speed and path distance to control variability.

## Slide 18
Reduces friction during assembly
Improves ergonomics and avoids injuries
Increases outputs and reduces rejects
Obtains closer fits
Safe and economical to use
Once dry, will not re-lubricate, even in the presence of water
Compatible with most surfaces
No petroleum distillates
No silicon or CFCs
Ready to use – no need to dilute
Benefits of P-80®

## Slide 19
WINDOW
EXHAUST
HANGERS
Typical Automotive Assembly Applications

## Slide 20
Typical Truck Assembly Applications
WEATHER SEALS (DOOR, WINDOW, CAB)
FUEL TANK STRAPS
5th WHEEL & BUSHINGS
TRANSMISSION COOLER LINES
EXHAUST HANGER ISOLATORS
AIR INTAKE HOSES
TIRE MOUNTING
WINDSHIELD WASHER HOSES & PUMPS
LUMBAR SUPPORT HOSES
VIBRATION BUSHINGS
SUSPENSION BUSHINGS
WIRE HARNESS-PULL
BRAKE LINES
HEATER HOSE

## Slide 21
BOOT ASSEMBLY
DRIVE SHAFT
Typical Rubber Assemblies

## Slide 22
SEAL ASSEMBLY
  Drive shaft
  Axle
Typical Rubber Assemblies

## Slide 23
HOSE FITTINGS
  Radiator
  Cooler
  Fluid lines
Typical Rubber Assemblies

## Slide 24
SEALS
DOOR SEALS
TRUNK SEALS
WINDOW SEALS
WEATHER STRIPING
Typical Rubber Assemblies

## Slide 25
P-80® lubricants should be stored at temperatures between 2°— 30° (36°— 86°F) in the original sealed container. Do not store outdoors in direct sunlight during warm weather.
For proper inventory control, use oldest material first. Each container has a lot number that gives the date (yymmdd) that the material was produced. For instance, lot number 140105 was produced in 2014 (14), during January (01), on the fifth day (05). If your plant personnel know this dating system, they can avoid using new material while older stock is available. For shelf life, please refer to the appropriate Safety Data Sheet.
Before dispensing P-80 Emulsion and P-80 Emulsion IFC from drums, stir with a mixing recirculation pump or folding propeller mixer for 5 to 10 minutes to ensure a homogenous mixture is drawn off. If a hold tank is used, agitate the lubricant before it is fed to assembly equipment. Smaller containers should be shaken or stirred prior to use. Never use air agitation on any P-80 product. Bubbling compressed air through P-80 lubricants may introduce bacteria that can overpower the preservatives causing separation or spoilage.
Store P-80 lubricants in a sealed container when not in use. Do not pour dispensed product back into the original container.
P-80 Emulsion IFC and P-80 THIX IFC meet the requirements of 21 CFR 178.3570, which controls lubricants for incidental food contact. Use the minimum amount of lubricant needed to lubricate the part. Apply it in a way that minimizes food contact.
All equipment and storage tanks, including transfer lines, containers, reservoirs, mixers, and pumps in contact with P-80 lubricants should be cleaned at least once a month using a mild detergent such as International Products’ LF2100® Liquid Low-Foam Cleaner or Micro-90® Concentrated Cleaning Solution. Rinse with potable water. Samples of each cleaner are available from International Products Corporation. Follow cleaning with a sanitizer rinse (see section B for details). This procedure is particularly important in hot or dirty work areas.
Do not mix P-80 with other chemicals.
Do not dilute P-80 with water.
Excess P-80 can be wiped or washed away with soap and water.
For safety details and shelf life, please refer to the appropriate Safety Data Sheets.
P-80® Storage and Handling

## Slide 26
PLASTIC | PROPERTY | 1 Day, %∆ |  |  |  |  | 10 Days, %∆ |  |  |  | 
 |  | P-80 Emulsion | P-80 Thix | P-80 Grip-It | P-80 Redi- Lube | Tap Water | P-80 Emulsion | P-80 Thix | P-80 Grip-It | P-80 Redi-Lube | Tap Water
ABS | %∆ Mass %∆ Hardness %∆ Swell | + 0.2 - 2.5 + 0.4 | + 0.2 - 1.4 + 0.5 | + 0.2 - 0.4 + 0.1 | + 0.3 - 3.3 + 0.1 | + 0.2 -0.6 - 0.1 | + 0.3 - 1.2 + 0.1 | + 0.4 - 3.7 + 0.7 | + 0.5 + 0.6 0.0 | + 0.1 - 1.4 - 0.2 | + 0.4 - 1.5 - 1.1
Polymethyl Methacrylate* | %∆ Mass %∆ Hardness %∆ Swell | + 0.1 - 1.1 0.0 | + 0.2 + 0.7 + 0.3 | + 0.2 - 1.1 0.0 | + 0.2 - 1.4 + 0.1 | + 0.1 - 0.7 0.0 | + 0.5 - 1.8 + 0.3 | + 0.7 0.0 + 0.1 | + 0.7 - 0.5 + 0.2 | + 0.7 - 0.5 + 0.2 | + 0.5 - 2.5 - 0.4
Acetal | %∆ Mass %∆ Hardness %∆ Swell | + 0.1 0.0 + 0.2 | + 0.1 0.0 0.0 | + 0.1 - 1.3 0.0 | + 0.1 - 0.2 + 0.1 | + 0.1 + 0.6 0.0 | + 0.3 - 0.9 + 0.5 | + 0.4 - 0.4 + 0.2 | + 0.3 - 1.1 + 0.3 | + 0.3 - 0.2 + 0.1 | + 0.4 - 2.1 + 0.1
HDPE | %∆ Mass %∆ Hardness %∆ Swell | 0.0 - 2.8 - 0.1 | 0.0 - 2.3 + 0.3 | 0.0 + 1.1 - 0.1 | 0.0 - 2.1 - 0.4 | 0.0 + 3.4 + 0.1 | 0.0 - 5.6 - 0.2 | 0.0 - 4.9 + 0.1 | 0.0 + 2.7 - 0.2 | 0.0 - 2.3 - 0.6 | 0.0 - 0.8 + 0.5
PETG | %∆ Mass %∆ Hardness %∆ Swell | + 0.1 - 1.8 - 0.3 | + 0.1 - 0.9 + 0.1 | + 0.1 + 0.4 - 0.1 | + 0.1 0.0 0.0 | + 0.1 - 0.4 + 0.1 | + 0.2 - 2.5 + 0.1 | + 0.3 - 2.1 + 0.1 | + 0.2 - 1.7 - 0.2 | + 0.2 - 1.9 + 0.1 | + 0.2 - 3.1 + 0.1
Polycarbonate* | %∆ Mass %∆ Hardness %∆ Swell | + 0.1 - 1.2 0.0 | + 0.1 - 0.4 - 0.1 | + 0.2 + 0.2 0.0 | + 0.1 - 0.4 0.0 | + 0.1 - 0.8 - 0.1 | + 0.1 - 1.9 + 0.2 | + 0.2 - 1.2 0.0 | + 0.1 - 1.2 0.0 | + 0.1 + 0.6 + 1.0 | + 0.1 - 0.6 0.0
Polyetherimide | %∆ Mass %∆ Hardness %∆ Swell | + 0.2 - 0.7 + 0.1 | + 0.2 - 0.2 + 0.1 | + 0.1 + 0.5 - 0.1 | + 0.2 - 0.4 + 0.3 | + 0.2 - 0.9 - 0.1 | + 0.5 - 1.1 + 0.4 | + 0.7 - 0.4 + 0.4 | + 0.5 0.0 + 0.1 | + 0.4 - 0.2 + 0.2 | + 0.5 - 0.9 - 1.5
Polypropylene | %∆ Mass %∆ Hardness %∆ Swell | 0.0 - 1.9 + 0.5 | 0.0 - 1.5 0.0 | 0.0 + 4.1 0.0 | 0.0 0.0 - 0.1 | 0.0 + 4.1 - 0.6 | + 1.0 - 1.7 + 0.1 | 0.0 - 0.4 + 0.2 | 0.0 + 4.1 0.0 | 0.0 - 1.3 - 0.1 | 0.0 + 2.0 - 0.7
PPO* | %∆ Mass %∆ Hardness %∆ Swell | 0.0 - 0.4 0.0 | 0.0 - 0.9 - 0.1 | 0.0 + 0.2 + 0.1 | 0.0 - 0.6 - 0.2 | 0.0 + 0.2 + 0.4 | + 0.1 - 0.4 0.0 | 0.0 - 1.3 0.0 | + 0.1 + 0.2 0.0 | 0.0 + 0.6 - 0.3 | + 0.1 + 0.4 0.0
PVC | %∆ Mass %∆ Hardness %∆ Swell | 0.0 - 0.6 + 0.4 | 0.0 - 1.1 0.0 | 0.0 + 1.0 0.0 | 0.0 + 0.2 - 0.2 | 0.0 - 0.8 - 0.4 | + 0.1 - 0.6 0.3 | 0.0 - 0.8 0.0 | 0.0 + 0.4 0.0 | + 0.1 + 0.6 - 0.3 | + 0.1 - 0.6 - 0.4
Polytetra-fluoroethylene | %∆ Mass %∆ Hardness %∆ Swell | 0.0 + 2.0 - 0.1 | 0.0 + 1.3 0.0 | 0.0 - 3.9 - 0.4 | 0.0 - 2.6 0.0 | 0.0 + 7.9 - 0.5 | 0.0 - 0.3 + 0.2 | 0.0 + 0.3 + 0.2 | 0.0 - 3.6 - 0.4 | 0.0 - 2.0 0.0 | + 0.1 + 1.8 - 0.4
Polyamide 6 | %∆ Mass %∆ Hardness %∆ Swell | + 0.6 - 1.6 + 0.5 | + 0.7 - 2.2 + 0.4 | + 0.6 - 2.7 + 0.6 | + 1.4 - 3.4 + 0.5 | + 0.6 - 1.7 + 0.3 | + 2.2 - 8.6 +1.4 | + 2.4 -12.8 + 1.3 | + 2.3 - 8.6 + 1.3 | + 2.6 -10.7 + 1.3 | + 2.2 -11.5 + 1.2
CONCLUSION: P-80 lubricants were found to be compatible with the plastics listed below when immersed for a total of ten days at room temperature.
Customers are encouraged to conduct their own tests before using P-80 lubricants.
METHOD Modified version of ASTM D543-95,
Practice A; Room Temp.
Mass: Analytical Balance, 0.0001 grams;
CoV – 4.0E-6%
Hardness: Shore D Durometer,
1 – 100 HD; CoV – 0.32%
Swell: Mitutoyo Micrometer, 0.001 mm,
CoV – 0.11%
KEY
ABS - Acrylonitrile butadiene styrene
HDPE - High Density Polyethylene
PETG - Polyethylene terephthalate
glycol-modified
PPO - Polyphenylene Oxide – Styrene
PVC - Polyvinyl chloride
*Under strain, these plastics may
show crazing.
P-80® Plastic Compatibility At Room Temperature

## Slide 27
P-80® Elastomer Compatibility At Room Temperature
ELASTOMER | PROPERTY | 1 Day, %∆ |  |  |  |  | 10 Days, %∆ |  |  |  | 
 |  | P-80 Emulsion | P-80 Thix | P-80 Grip-It | P-80 Redi- Lube | Tap Water | P-80 Emulsion | P-80 Thix | P-80 Grip-It | P-80 Redi- Lube | Tap Water
Buna N | %∆ Mass ∆ Hardness, pts %∆ Swell | + 0.2 + 1.8 0.0 | + 0.2 + 0.2 - 0.3 | + 0.2 - 1.0 + 0.9 | + 0.9 - 1.0 + 0.1 | + 0.1 + 1.2 + 0.1 | + 0.9 + 0.5 - 0.2 | + 0.8 - 1.5 - 0.3 | + 0.7 - 1.2 + 0.1 | + 3.5 - 3.0 + 2.2 | + 0.2 + 2.7 - 0.8
Butyl | %∆ Mass ∆ Hardness, pts %∆ Swell | + 0.1 + 0.7 + 0.1 | + 0.1 - 0.7 + 0.5 | 0.0 - 4.3 - 0.1 | + 0.5 - 2.0 + 0.3 | 0.0 - 0.3 + 0.2 | + 0.4 - 2.1 - 0.5 | + 0.5 - 1.7 + 0.7 | + 0.2 - 1.2 - 1.1 | + 2.1 - 1.7 + 2.2 | + 0.1 - 0.5 - 0.2
ECH | %∆ Mass ∆ Hardness, pts %∆ Swell | + 0.4 - 0.7 - 0.5 | + 0.6 - 0.3 - 0.3 | + 0.7 - 4.0 - 0.1 | + 1.1 + 0.5 + 0.1 | + 0.4 + 4.7 + 0.3 | + 1.1 - 4.0 - 0.2 | +1.2 - 4.3 - 0.2 | + 2.2 - 1.3 + 0.6 | + 2.2 - 1.0 + 0.4 | + 1.4 + 4.8 + 0.8
EPDM | %∆ Mass ∆ Hardness, pts %∆ Swell | + 0.1 - 1.8 + 0.2 | + 0.1 - 2.3 - 0.3 | 0.0 - 3.7 + 0.4 | + 0.7 - 0.8 + 0.2 | 0.0 - 1.5 - 0.8 | 0.0 - 2.5 + 0.2 | + 0.6 - 5.3 - 0.2 | + 0.2 - 4.5 + 0.8 | + 2.6 - 1.8 + 0.9 | + 0.1 - 3.3 - 0.8
Natural Gum Rubber | %∆ Mass ∆ Hardness, pts %∆ Swell | + 0.1 - 1.8 - 0.1 | + 0.2 - 1.2 - 0.7 | + 0.4 - 2.2 + 0.5 | + 0.9 - 0.8 + 0.7 | + 0.1 + 1.3 + 0.0 | + 0.8 - 1.3 - 0.2 | + 1.2 - 3.3 - 0.6 | + 1.5 - 3.0 + 0.7 | + 4.4 - 3.8 + 1.7 | + 0.2 - 0.7 + 0.1
Neoprene | %∆ Mass ∆ Hardness, pts %∆ Swell | + 0.2 - 2.2 - 0.1 | + 0.3 + 0.5 + 0.3 | + 0.4 - 2.7 + 0.8 | + 1.1 - 2.3 0.0 | + 0.1 - 1.7 + 0.1 | + 1.2 - 4.7 + 0.8 | + 1.4 - 3.7 + 0.6 | + 1.5 - 4.7 + 1.1 | + 4.3 - 6.5 + 2.8 | + 0.5 - 3.5 - 0.1
SBR | %∆ Mass ∆ Hardness, pts %∆ Swell | + 0.2 - 2.8 + 0.1 | + 0.3 - 0.2 + 0.3 | + 0.2 - 2.2 - 0.1 | + 1.1 - 2.3 + 1.4 | + 0.1 + 4.0 + 0.1 | + 1.0 - 9.0 + 1.5 | + 1.2 - 2.0 + 1.2 | + 0.6 - 5.8 + 0.5 | + 4.2 - 7.8 + 5.2 | + 0.2 + 1.8 + 0.1
Silicone | %∆ Mass ∆ Hardness, pts %∆ Swell | + 0.3 - 2.2 - 0.1 | + 0.2 +0.2 + 0.6 | + 0.1 + 1.0 0.0 | + 1.2 - 4.1 + 0.2 | 0.0 + 0.7 + 0.4 | + 0.9 - 1.3 + 0.7 | + 1.0 - 0.3 + 0.9 | + 0.6 + 5.3 + 0.3 | + 4.9 + 4.2 + 5.0 | 0.0 - 0.7 + 0.6
Viton | %∆ Mass ∆ Hardness, pts %∆ Swell | + 0.1 - 2.2 - 0.1 | + 0.1 - 1.3 - 0.3 | 0.0 - 1.0 + 0.5 | + 0.1 - 3.8 - 0.5 | 0.0 + 1.3 - 0.1 | + 0.2 - 2.7 - 0.5 | + 0.3 - 3.0 0.0 | + 0.2 - 3.5 + 0.4 | + 1.1 - 1.8 + 0.8 | + 0.1 - 0..5 + 0.6
CONCLUSION: While there are no standard specifications for excessive swell and hardness data, minimal changes are regarded as between
-5 to +20% and -5 to +10 points, respectively1. (Vecchio, 2001) Based on these criteria, P-80 lubricants have acceptable swell and hardness compatibility
results after 10 days. Mass compatibility results are favorable compared to the tap water control samples.
Customers are encouraged to conduct their own tests before using P-80 lubricants.

## Slide 28
METAL | PROPERTY | 1 Day, %∆ |  |  |  |  | 14 Days, %∆ |  |  |  | 
 |  | P-80 Emulsion | P-80 Thix | P-80 Grip-It | P-80 Redi- Lube | Tap Water | P-80 Emulsion | P-80 Thix | P-80 Grip-It | P-80 Redi- Lube | Tap Water
ALUMINUM 1100 | %∆ Mass | 0.00 | 0.00 | - 0.15 | - 0.01 | 0.00 | 0.00 | 0.00 | - 0.44 | - 0.02 | - 0.05
 | ∆ Appearance | No change | No change | Darker overall | No change | Several pinpoints | No change | No change | Black | No change | Pinpoints
*BRASS ALLOY 260 | %∆ Mass | - 0.01 | - 0.35 | - 0.04 | - 0.01 | 0.00 | - 0.02 | - 0.36 | - 0.47 | - 0.02 | 0.00
 | ∆ Appearance | No change | Dull finish | Faded Appearance | No change | Dark spots | Faded appearance | Darker outlines | Faded appearance | Dark spots | Dark spots
*BRONZE ALLOY 220 | %∆ Mass | - 0.01 | - 0.01 | - 0.04 | - 0.01 | 0.00 | - 0.02 | - 0.02 | - 0.50 | - 0.03 | 0.00
 | ∆ Appearance | No change | No change | Faded appearance | No change | Dark spots | Faded appearance | Dark spots | Faded appearance | Dark spots | Dark spots
1008 COLD ROLLED STEEL | %∆ Mass | 0.00 | 0.00 | - 0.01 | 0.00 | - 0.04 | 0.00 | 0.00 | - 0.06 | - 0.01 | - 0.47
 | ∆ Appearance | No change | No change | No change | No change | No change | No change | No change | Pinpoints | No change | Rust spots
*COPPER ALLOY CA 110 | %∆ Mass | - 0.01 | - 0.01 | - 0.05 | - 0.01 | 0.00 | - 0.02 | - 0.02 | - 0.51 | - 0.01 | 0.00
 | ∆ Appearance | No change | No change | Faded appearance | No change | Darker outlines | Faded appearance | Dark spots | Faded appearance | Dark spots | Darker outlines
MONEL 400 | %∆ Mass | 0.00 | 0.00 | 0.00 | 0.00 | 0.00 | - 0.01 | - 0.01 | 0.00 | - 0.01 | 0.00
 | ∆ Appearance | No change | No change | No change | No change | No change | No change | No change | No change | No change | No change
304 STAINLESS STEEL | %∆ Mass | 0.00 | 0.00 | 0.00 | 0.00 | 0.00 | - 0.01 | 0.00 | 0.00 | 0.00 | 0.00
 | ∆ Appearance | No change | No change | No change | No change | No change | No change | No change | No change | No change | No change
TITANIUM ALLOY, 8% Mn | %∆ Mass | 0.00 | 0.00 | 0.00 | 0.00 | 0.00 | 0.00 | - 0.01 | 0.00 | 0.00 | 0.00
 | ∆ Appearance | No change | No change | No change | No change | No change | No change | No change | No change | No change | No change
Customers are encouraged to conduct their own tests before using P-80 lubricants.
Underlined = Not Recommended *P-80 RESIDUE WILL DISCOLOR COPPER AND COPPER ALLOYS.
P-80® Metal Compatibility At Room Temperature

## Slide 29
Contact us for product information and samples or a copy of this presentation International Products Corporation USA Headquarters 201 Connecticut Drive Burlington NJ 08016 USA Tel. 609-386-8770 Fax. 609-386-8438
Kathy Wyrofsky, President 609-386-8770 x213 kwyrofsky@ipcol.com
Tom McGuckin, VP Research and Quality 609-386-8770 x210 tmcguckin@ipcol.com
Michele Christian, Marketing Director 609-386-8770 x222 mchristian@ipcol.com
Judy Shapiro, Account Specialist 609-386-8770 x 217 jshapiro@ipcol.com
Website: www.ipcol.com U.K. Branch Unit 5 Green Lane Business Park 238 Green Lane - London SE9 3TL U.K. Tel. 0208 857 5678 Fax. 0208 857 1313 saleseurope@ipcol.com
Thank you!